|  | INCH-POUND |
| --- | --- |

MIL-PRF-MCLWES

30 January 2009

PERFORMANCE SPECIFICATION

Lightweight Exposure Suit

U.S. MARINE CORPS

The United States Marine Corps has approved this document for use.

1. SCOPE.

1.1 Scope.  This document covers the requirements for the Marine Corps lightweight exposure jacket and trouser for wind and rain protection in mountain conditions.

1.2 Schedule of sizes. The jacket and trouser shall be constructed in the following sizes (see 6.2).

SMALL	MEDIUM	LARGE	XLARGE

Short		Short

Regular	Regular	Regular

Long		Long		Long

Beneficial comments (recommendations, additions, and deletions) and any data that may improve this document should be addressed to: Marine Corps Systems Command (MARCORSYSCOM) 2202 Lester Street, Quantico, VA 22134-5000.

AMSC N/A									FSC  8415

DISTRIBUTION STATEMENT A.  Approved for public release; distribution is unlimited

2.  APPLICABLE DOCUMENTS

2.1 General.  The documents listed in this section are specified in sections 3 and 4 of this specification.  This section does not include documents cited in other sections of this specification or recommended for additional information or as examples.  While every effort has been made to ensure the completeness of this list, document users are cautioned that they must meet all specified requirements cited in sections 3 and 4 of this specification, whether or not they are listed.

2.2  Government documents.

2.2.1 Government documents, drawings, and publications.  The following Government documents, drawings, and publications form a part of this document to the extent specified herein.  Unless otherwise specified, the issues are those specified in the solicitation.

SPECIFICATIONS

COMMERCIAL ITEM DESCRIPTIONS

A-A-50199		Thread, Poly Core: Cotton- or Polyester-Covered

A-A-55634		Zippers (Fasteners, Slide Interlocking)

A-A-55126		Fastener Tape, Hook and Loop, Synthetic

A-A-50083		Bag, Plastic, Folded Garment

MILITARY

MIL-T-3530		Thread and Twine Mildew Resistant or Water Repellent Treated

MIL-DTL-32075	Label: for clothing, Equipage and Tentage (General Use)

MIL-PRF-5038	Tape, Textile and Webbing, Textile, Reinforcing Nylon

MIL-F-10884		Fasteners, snap

MIL-E-20652		Eyelets

2.2.2  Other Government documents, drawings, and publications.  The following other Government documents, drawings, and publications form a part of this document to the extent specified herein.  Unless otherwise specified, the issues are those specified in the solicitation or contract.

Drawing Number	                    Drawing Description		                     	     Drawing Date

| 2-1-2529 | Desert MARPAT- 4 color (Light Tan 479) | 12-Jul-2004 |
| --- | --- | --- |
| 2-1-2530 | Desert MARPAT- 4 color (Urban Tan 478) | 12-Jul-2004 |
| 2-1-2531 | Desert MARPAT- 4 color (Light Coyote 481 with EGA symbol) | 12-Jul-2004 |
| 2-1-2532 | Desert MARPAT- 4 color (Highland 480) | 12-Jul-2004 |

(Copies of drawings are available from the U.S. Army Research, Development & Engineering Command, Natick Soldier Center, ATTN: AMSRD-NSC-IP-D, Natick, MA 01760)

2.3 Non-Government publications.  The following document(s) form a part of this document to the extent specified herein.  Unless otherwise specified, the issues of the documents not listed in the DODISS are the issues of the documents cited in the solicitation (see 6.2).

AMERICAN SOCIETY FOR TESTING AND MATERIALS

ASTM-D-751		Coated Fabrics

ASTM-D-2582	Puncture Propagation Tear Resistance of Plastic Film and Thin Sheeting

ASTM-D-3776 	Mass Per Unit Area (Weight) of Fabric

ASTM-D-5034	Breaking Strength and Elongation of Textile Fabrics (Grab Test)

ASTM-D-6193 	Stitches and Seams

ASTM-E-96		Water Vapor Transmission

ASTM-F-392		Flex Durability of Flexible Barrier Materials

(Copies should be obtained from the American Society for Testing and Materials, 100 Barr Harbor Drive, West Conshohocken, PA 19426-2959).

AMERICAN ASSOCIATION OF TEXTILE COLORIST AND CHEMISTS

AATCC- 8 		Colorfastness to Crocking; Crockmeter Method

AATCC -16 		Colorfastness to Light

AATCC-22 		Spray Rating

AATCC-61 		Colorfastness to Laundering, Home and Commercial; Accelerated

AATCC-70 		Dynamic Absorption

AATCC-96		Dimensional Changes in Commercial Laundering of Woven and Knitted

Fabrics Except Wool

AATCC-135 		Dimensional Changes in Commercial Laundering of Woven and Knitted

Fabrics Except Wool

AATCC Evaluation Procedure 6 – Instrumental Color Measurement

AATCC Evaluation Procedure 9 – Visual Assessment of Color Difference of Textiles

MISCELLANEOUS

ANSI/ASCQ Z1.4- Sampling Procedures and Tables for Inspection of Attributes

(Applications for copies should be addressed to the American National Standards Institute, 1430 Broadway, New York, NY 10018-3308.)

2.4 Order of precedence.  In the event of a conflict between the text of this document and the references cited herein, the text of this document takes precedence.  Nothing in this document however, supersedes applicable laws and regulations unless a specified exemption has been obtained.

3. REQUIREMENTS

3.1  First article.  When specified, (see 6.2), a sample shall be subjected to first article inspection (see 6.3), in accordance with 4.2.

3.2  Recycled, recovered, or environmentally preferable materials.  Recycled, recovered, or environmentally preferable materials should be used to the maximum extent possible provided that the material meets or exceeds the operational and maintenance requirements, and promotes economically advantageous life cycle costs.

3.3 Design and construction.

3.3.1 Design. The jacket and trouser shall be lightweight, low volume, and water vapor permeable to minimize overheating from strenuous activities. All exposed stitching construction shall be waterproof for the life of the garment, while meeting the finished weight and volume.  Bartack reinforcements shall be provided at zipper pulls. Hook fasteners shall be extruded style to minimize icing and lint build-up. Each garment shall be labeled to identify the item, its size, and use and care. The size label shall be easily found and attached below the center back neckline and waist.  The jacket and trouser shall comply with Propper International Product number F7401-87-929 for the jacket, product number F7201-87-929 for the trouser using W.L. Gore GORE-TEX®   Paclite®, or equal, as defined by the performance specification and illustrations provided.

3.3.2 Basic material. The outershell material for the jacket and trouser shall be waterproof and moisture vapor permeable, constructed with a 100% nylon shell fabric, W.L. Gore GORE-TEX® Paclite® laminate, or equal.  The shell material shall be waterproof and windproof. The outershell material shall be quick drying when it become wet or damp and shall be durable to repeated launderings.   The fabric shall conform to the requirements in Table I; minimum performance characteristics of the fabric are based upon an average of 5 determinations.

Table I. Physical Properties

| Physical Property | Requirement | Test Method |
| --- | --- | --- |
| Tear Strength: warp x filling | 2.0 x 2.5 kgf, min | ASTM D- 2582 where tear shall be straight on face of fabric |
| Break Strength: warp x filling | 100 x 100, lbs., min | ASTM D- 5034 (GE or GT) |
| Resistance to Organic Liquids after 5 launderings | Rating B (min) | AATCC 135 1/ and one drop of n-tetradecane for 30 seconds |
| Spray Rating after 5 launderings | 100,90,90 min | AATCC 135 1/ and AATCC-22 |
| Water Permeability Fabric Seams After Accelerated Aging After –20 F Flex Fatigue: warp x filling After physical surface appearance After synthetic perspiration Blocking | No leakage No leakage No leakage No leakage No leakage No leakage Rating 1 (min) | ASTM D-751-06 (Procedure B2, 41-44 except fixed 50 cm water column/10 min) ASTM D-751-06: 72-79, followed by Procedure B2,41-44 except fixed 50 cm water column/10min.Aging conditions shall be 160 deg F for 7 days ASTM F-392 (1000 cycles) & ASTM D-751-06 (Procedure B2,41-44) 4/ & ASTM D-751-06 (Procedure B2, 41-44 except fixed 50 cm water column/10 min) 2/ & ASTM D-751-06 (Procedure B2, 41-44 except fixed 50 cm water column/10 min) ASTM D-751-06:49-53 except 180 +/- 2 deg F for 30 minutes |
| Dimensional Stability: Warp x filling | 4.0 % x 2.0 % max | AATCC–96, Option 1C |
| Hydrostatic Resistance Initial After strength of coating After High Humidity | 100 psi; min 90 psi; min 90 psi; min | ASTM D-751 (Procedure A, 37-40) water pressure applied to face side. ASTM D-751-06:49-53 except separation rate at 12 in/min and load of 20 lbs. ASTM D-751-06:72-79 (Desiccator with water in oven at 160 deg F for 7 days.) |
| Diethyltoluamide (DEET) Initial and after 5 launderings | 90 psi; min | Contaminate per 3/, laundered per AATCC 135 1/ and test per ASTM D-751 (Procedure A, 37-40) |
| Moisture Vapor Transmission | B 650 g/m2/24hr, min BW 4500 g/m2/24hr, min | 6/ASTM E 96 B 6/ASTM E 96 Procedure BW |

1/ Laundering method AATCC 135 with AATCC Detergent (non-phosphate, warm water at 100 -110 def F for 30 minutes and tumble dry, permanent press cycle 150 – 160 deg F.  To prevent residual detergent, the 5th cycle shall be run without detergent.

2/ Synthetic perspiration test.  The specimen, 8-inches, shall be cut and exposed to synthetic perspiration as follows:  The synthetic perspiration solution shall be made by combining 3.0 grams sodium chloride, 1.0 gram trypticase soy broth powder, 1.0 gram normal propyl propionate, 0.5 gram of liquid lecithin and 500 ml of distilled water.  Cover the solution and stir while heating to 50oC until all ingredients are dissolved.  Then, cool the solution to 35oC, remove cover and dispense it immediately with a pipette or other suitable measuring device.  Dispense 2 ml of perspiration solution at 35oC onto the center of an 8-inch by ¼-inch glass plate.  Place the specimen on the glass plate with the back side contacting the glass.  Dispense an additional 2 ml of synthetic perspiration solution onto the center of the specimen.   Place a second 8-inch by 8-inch by ¼-inch glass plate on top of the specimen and then place a 4-pound weight on top of and in the center of the assembly.  After 16 hours, remove the specimen (do not rinse) and air dry the specimen before testing.

3/ DEET contamination: 3 drops of 75%diethyltoluamdie/25% ethanol shall be applied to the center of 4” x4” specimen.  A glass plate shall be placed on specimen with a pressure of 0.25psi for 16 hours.  After conditioning the sample shall be immediately removed and hydrostatic resistance shall be measured.

4/Conduct twenty (20) launderings and drying cycles in accordance with 5/. Each sample 48 inches in length by full width, shall be cut in half across the width of cloth. One half of the sample (24 inch in length) shall be laundered and the remaining half retained as the unlaundered portion for the final evaluation, as necessary.   After each drying cycle, examine both sides of the cloth for changes in physical surface appearance when compared to the unlaundered sample.

5/ Laundering procedure. .  Place 2.0 +/- 0.2 pounds of cloth and, if needed, ballast in an automatic washing machine set on permanent press cycle, high water level and warm (1000 F+/- 10 0 F) wash temperature. Place 0.5 ounce (14 grams) of 1993 AATCC Standard Reference Detergent (non-phosphate) without optical brighteners into the washer.  The duration of each laundering cycle shall be 30 +/- 5 minutes.  After laundering place sample and ballast in an automatic tumble dryer set on permanent press cycle, 1500-1600F, and dry for approximately 15 minutes. The laundering equipment, washer and dryer, shall be in accordance with AATCC-135.

6/ Moisture Vapor Transmission Rate.  ASTM E-96 with temperature and humidity conditions of 73.5o + 1oF and 50 + 2% R.H.  The linear air flow velocity in the wind tunnel shall be set to yield an upright, ‘open cup’ evaporation rate at all test specimen positions of 15000 + 1000 g/m2/24h (The evaporation rate shall be determined by conducting an upright cup, Procedure B test (see 4.6.1.1), without a test specimen for a period of exactly two (2) hours).  For specimen testing using Procedure BW, the ‘open cup’ evaporation rate shall be determined in the air stream at a level not more than three (3) inches below the position of the inverted cup test specimen.

3.3.3 Reinforcement Material. The reinforcement cloth for the seat patch, knee patch, and elbow patch shall be  61 x 40 plain weave 330 denier Cordura® (or equal)100% Nylon warp and filling, water repellent treated, resistant to fraying, Desert MARPAT printed and shall match the visual shade of the outershell fabric.

3.3.4 Color matching.

3.3.4.1 Visual matching (all types and classes).  The color and appearance of the cloth shall match the standard sample when viewed using AATCC Evaluation Procedure 9, Option A, under filtered tungsten lamps that approximate artificial daylight D75 illuminant with a color temperature of 7500 ( 200 K with illumination of 100 ( 20 foot candles, and shall be a good match to the standard sample under horizon lamplight at 2300 ( 200 K.

3.3.4.2 Instrumental color matching (all types and classes).  Instrumental color matching is used as a tool to quantify shade evaluation if visually shade is rated unacceptable.  The fabric shall be instrumentally measured and shall match the standard sample as specified in 4.4.3 for evaluation procedure and acceptance requirements.

3.3.5 Colorfastness (all types and classes).  The finished cloth shall show fastness to: light (after 40 AATCC standard fading hours or 170 Kilojoules); laundering (after 3 cycles); and crocking.  The colorfastness of the cloth shall be equal to or better than the standard sample, or equal to or better than a rating of “3-4” using the AATCC Gray Scale for Color Change and a rating of “3-4” using the AATCC Gray Scale for Staining for each of the colors. The finished cloth shall show colorfastness equal to or better than the standard sample for all colors when tested as specified in 4.4.1.1.

3.3.6 Color. The garment materials shall be MARPAT desert camouflage print.  The exterior material(s) shall meet reflectance requirements specified in Table III when tested in accordance with AATCC Evaluation Procedure 6 and 9.  No shaded parts are allowed on garment exterior. All fabrics shall provide show good colorfastness (rating 3-4) to crocking, light, and laundering when tested in accordance with AATCC Methods 8, 16 and 61, respectively.

3.3.7 Spectral reflectance. The finished outershell cloth shall meet the spectral reflectance values (in percent) for the visible/near infrared wavelength range, 600 to 860 nanometers (nm) for the colors specified in Table II as applicable when tested as specified in 4.4.2.

#### Table II. Spectral Reflectance

| Wavelengths | Lt. Tan 479 | Lt. Coyote 481 & Highland 480 | Urban Tan 478 |
| --- | --- | --- | --- |
| Nanometers | Min. | Max. | Min. | Max. | Min. | Max. |
| 700 | 38 | 53 | 19 | 41 | 25 | 44 |
| 720 | 38 | 54 | 20 | 41 | 25 | 45 |
| 740 | 39 | 55 | 20 | 42 | 25 | 46 |
| 760 | 40 | 56 | 21 | 42 | 26 | 47 |
| 780 | 41 | 57 | 21 | 42 | 27 | 48 |
| 800 | 43 | 58 | 22 | 43 | 28 | 50 |
| 820 | 45 | 59 | 23 | 45 | 30 | 52 |
| 840 | 48 | 62 | 24 | 46 | 33 | 55 |
| 860 | 50 | 65 | 25 | 48 | 36 | 58 |

3.3.8. Components.

3.3.8.1. Jacket zippers. Zipper closures for the center front, armpit, sleeve pocket, and front pocket pass-through shall be easily pulled with gloved hand and zipper flaps shall be included on the jacket pass thru opening, center front shall have a back flap. Zipper shall be black or a brown shade that matches the desert print (coyote preferable) and shall be as follows:

1. Front zipper shall be in accordance to A-A-55634, continuous element size 8 REVERSE coated chain, Type III, Style 8, single autolock slider except it shall operate reverse side with black 2.5 mil thick (min) water-resistant polyurethane coated zipper tape facing out and capable to seam tape on inner tape side. Slider pull shall have hole large enough to accommodate thong. Brand name YKK style CNT4OL-86 DABL 5/8 URETEK or equal.

2. Chest opening and armpit zippers shall be the same except they shall be size 5 with pull holes large enough to accommodate thong.

3. Sleeve pockets are standard coil and closed on both ends.   Brand name YKK style CNFC-56 DABLHD BTM2 or equal.

Each slide fastener shall be equipped with a 3/8 inch wide thong in accordance to A-A-55634.  The thong shall measure 3 inches folded and shall be secured with a bartack.

3.3.8.2 Trouser zippers. Zipper closures for front fly, pocket pass thru and outseam shall be easily pulled with gloved hand and zipper flaps shall be included on the fly, and pocket pass thru.  Outseam zippers shall have a back flap for protection.  Zippers shall be black or a brown shade that matches the desert print (coyote preferable) and shall be as follows:

1. Fly zipper in accordance with A-A-55634,  Type I, Style 4, size 5 coil chain with water repellant treated tape(non coated), single autolock slider with pull hole large enough to accommodate thong. Brand name YKK style CNFC-56 DALHD E 5/8 or equal.

2. Lower leg zippers shall  be the same as the front jacket zipper except Type I, Style 4, size 5 REVERSE coil chain with water repellent treated tape, non coated, and pull hole large enough to accommodate thong. Brand name YKK style CNFC-56 DABLHD E 5/8 P-TOP P-BTM REVERSE or equal.

3. Side pass through shall be water repellent treated tape (non coated), single autolock slider with pull hole large enough to accommodate thong, closed on both ends. Brand name YKK style CNT4C-56DABLHD BTM2 REV or equal.

Each slide fastener shall be equipped with a 3/8 inch wide thong in accordance to A-A-55634.  The thong shall measure 3 inches folded and shall be secured with a bartack.

3.3.8.3 Pocketing.  Sleeve pockets shall be constructed with pocket flaps located at the top of each pocket.  Flaps shall lie flat without curling edges and remain secure, pockets shall have a self-drainage capability.

3.3.8.4 Fastener Tape, Hook and Loop.  The hook and loop fastener for the jacket and trouser shall be coyote tan.  The hook tape shall be extruded style to minimize icing and lint build-up and shall conform to A-A-55126, Class 4, type IV, Velcro part number HTH 745 or equal.  Loop fastener tape shall conform to A-A-55126, Class 4, type I, Velcro part number 1100 or equal.  Edges shall be finished so they do not ravel for the life of the garment. Stitching shall not be closer than 3/16 inch to a selvage edge.

3.3.8.5 Jacket Drawcords. The hood opening and jacket bottom hem shall have elasticized drawcords.  The elastic shall be 1/8” tubular.   The barrel locks (ITW Nexus, part #350-3000 or equal) shall have no free hanging ends, to easily adjust fit, close to the body, while wearing leather gloves.  The hem drawcord shall be located at the underside of side seam to avoid snagging. The Jacket waist drawcord shall have four eyelets; insert drawcord through tunnel and eyelets and add cannon clip, barrel lock and 3/8 inch Nylon Tape.

3.3.8.6 Thread.  The thread shall be Tex 40, 2 or 3 ply poly/cotton conforming to A-A-50199, and shall be water-repellent treated as specified in MIL-T-3530.

3.3.8.7 Snap Fasteners.  The snap fasteners for the trouser shall conform to style 2 finish 2 of MIL-F-10884.

3.3.8.8 Tape Nylon.  The nylon tape for the Jacket waist shall be 3/8 inch nylon tape and shall conform to type III of MIL-PRF-5038.

3.3.8.9 Eyelet/Washer.  The eyelet shall be brass and shall conform to MIL-E-20652 Stimpson Part No. A2358 and washer brass Stimpson Part No C669.  The color shall be black.

3.3.8.10 Elastic.  The elastic shall be 1 inch wide and shall be polyester 140 Stretch Knitted.

3.3.8.11 Cannon Clip. The clip shall be ITW Nexus part #743-0125 or equal.

3.3.8.12 Mini-Mesh.  The collar lining for the Jacket shall be 100% Nylon Mesh, Jason Mills style no. 6900 or equal, 3 oz  per square yard +/- 10% with a burst strength of 120 pounds.  Colorfastness to a 4.0 min (gray scale).

3.4 Labels.  Each jacket and trouser shall have a combination identification-size label, and instruction label.  The identification-size label shall contain the item description, contract number, size, NSN, fiber content information and the contractor’s name.  The label color shall be white.  The inscription shall have a minimum font size of 10 points.  The inscription legibility, label, and label attachment method shall last the expected life of the uniform.  The labels shall show fastness to laundering.  The labels must boldly specify size, identify the item, and provide use and care instructions.  Labels shall conform to requirements in MIL-DTL-32075.

3.4.1 Jacket Identification-size label. The label shall be located on the upper center back of the jacket.  The identification-size label shall contain the following information, as applicable:

Identification Information

JACKET, LIGHTWEIGHT EXPOSURE

CONTRACT NO.:

CONTRACTOR’S NAME:

Jacket Size Label Information

| Small Short Chest: Up to 37 in. Height: 63 to 67 in. NSN: 8415 01 555 1416 | Small Regular Chest: Up to 37 in. Height: 67 to 71 in. NSN: 8415 01 555 1425 |  |
| --- | --- | --- |
| Medium Short Chest: 37 to 41 in. Height: 63 to 67 in. NSN: 8415 01 555 1431 | Medium Regular Chest: 37 to 41 in. Height: 67 to 71 in. NSN: 8415 01 555 1434 | Medium Long Chest: 37 to 41 in. Height: Greater than 71 in. NSN: 8415 01 555 1437 |
|  | Large Regular Chest: 41 to 45 in. Height: 67 to 71 in. NSN: 8415 01 555 1447 | Large Long Chest: 41 to 45 in. Height: Greater than 71 in. NSN: 8415 01 555 2957 |
|  |  | X-Large Long Chest: 45 to 49 in. Height: Greater than 71 in. NSN: 8415 01 555 1452 |

3.4.2 Trouser Identification-size label. The label shall be located centered on the back waist of the trousers.  The identification-size label shall contain the following information, as applicable:

Identification Information

TROUSER, LIGHTWEIGHT EXPOSURE

CONTRACT NO.:

CONTRACTOR’S NAME:

Trouser Size Label Information

| Small Short Waist: Below 31 in. Inseam: 26-1/2 to 29-1/2 in. NSN: 8415 01 555 3009 | Small Regular Waist: Below 31 in. Inseam:29-1/2 to 32-1/2 in. NSN: 8415 01 555 3013 |  |
| --- | --- | --- |
| Medium Short Waist: 31-35 in. Inseam: 26-1/2 to 29-1/2 in. NSN: 8415 01 555 3016 | Medium Regular Waist: 31-35 in. Inseam: Up to 32-1/2 in NSN: 8415 01 555 3019 | Medium Long Waist: 31-35 in. Inseam: Over 32-1/2 in. NSN: 8415 01 555 3022 |
|  | Large Regular Waist: 35-39 in. Inseam: Up to 32-1/2 in. NSN: 8415 01 555 3026 | Large Long Waist: 35-39 in. Inseam: Over 32-1/2 in. NSN: 8415 01 555 3034 |
|  |  | X-Large Long Waist: Over 39 in. Inseam: Over 32-1/2 in. NSN: 8415 01 555 3028 |

3.4.3 Instruction label. The instruction label for the jacket and trouser shall conform to Type VI, Class 3 of MIL-DTL-32075, and shall include the following information:

Jacket Instruction Label Contents

- Hood should be stowed when not in use.

- Brush off snow and frost before entering heated shelters.

3.  Machine/hand washing.  Use Permanent Press Cycle.  Wash in warm water and use
    mild detergent.  Slide fasteners, hook and loop tape, and snap fasteners shall be

closed for wash and dry.

4. Tumble dry (cotton setting) or hang to dry on a rust proof hander.

DO NOT REMOVE THIS LABEL

Trouser Instruction Label Contents

- Brush off snow and frost before entering heated shelters.

2.  Machine/hand washing.  Use Permanent Press Cycle.  Wash in warm water and use
    mild detergent.  Slide fasteners, hook and loop tape, and snap fasteners shall be

closed for wash and dry.

3. Tumble dry (cotton setting) or hang to dry on a rust proof hanger.

DO NOT REMOVE THIS LABEL

3.4.4 Combination identification-size-instruction label.  As an alternate, a combination identification-size-instruction label may be used conforming to Type VI, Class 14 of MIL-DTL-32075.

3.5 Label/tag.  Each jacket and trouser shall have an individual bar code placed on a paper tag for personal clothing items.  The paper tag shall be standard bleached sulfate having a basis weight of 100 pounds.  The paper used for the tags shall have a smooth finish to accept thermal transfer and direct printing.  The tags shall have a hole and shall be attached to each item by a fastener.  The tags shall be clearly legible and readable by a scanner.  Label/tag shall conform to Type VIII, class 17 of MIL-DTL-32075.

3.6 Patterns. Patterns will not be furnished to the contractor.

3.7 Configuration.  The following specifics are needed to ensure uniform appearance, comfort and durability in garrison use, combat, and field operations.  End item construction and appearance shall conform to the requirements of this document, garment characteristics specified in Table III, and the finished dimensions as specified in Table V to maintain item configuration and compliance to end item and component performance tests (See 4.4).

Table III. Garment Characteristics

| Garment Characteristic | Requirement | Test Method |
| --- | --- | --- |
| Jacket Finished Weight and Volume Size Medium Regular | 1.15 lbs (max) 1/ | Scale weight to nearest 0.1 lbs. |
| Trouser Finished Weight and Volume Size Medium Regular | 0.95 lbs (max) 1/ | Scale weight to nearest 0.1 lbs. |
| Jacket Packed Volume Size Medium Regular | 195 cu in (max) | 2/ |
| Trouser Packed Volume Size Medium Regular | 160 cu in (max) | 2/ |

1/ End item weight and volume based upon an outer shell material  weight  not to exceed  3.7 oz/sq yd.  Other sizes weight and volume shall be proportional.

2/ Volume test method: Use constant rate of extension (Instron), 3/8” Lexan box measuring 12 ¾” W x 12” H and comparable size perforated top plate plunger (Contracting agency will provide detailed drawings of box). Mount plunger to the load cell such that the plunger stays parallel to the bottom surface of the box.  Set the initial position of the plunger by aligning the bottom face to the top edge of the box.  Insert the test sample in the box in whatever orientation desired and center the box with the plunger.  Compress the sample with a constant crosshead movement of 15 inches per minute or slower.  The test should be run at least until  45 lbf  is reached.  The packed volume is then calculated from the cross head travel formula below.  The sample shall then be removed from the box and fluffed prior to repeating the test.  The test shall be repeated five (5) times and the data shall be averaged.

Volume [cubic inches]= (initial volume [cubic inches])-144*(crosshead travel [inches])

The following Manual Method is acceptable if results are within 2% of the requirement.

Insert the test sample in the box in whatever orientation is desired and place the plunger in the box on top of the sample.  Slowly add weights until the 45lbf load is reached.  The weights shall not touch the sides of the box.  If any of the weights are released rapidly, the test shall be nullified.  Once the desired weight has been applied, measure from the top of the box to the top of the plate in each corner and average the four, and the thickness of the plunger to obtain the mean compression depth.  Calculate the packed volume from the previous equation, substituting the compression depth for the crosshead travel.

3.7.1 End Item Features

3.7.1.1 Jacket End Item Features (See Figure 1). The hood shall be attached and stowed in the collar, it shall not cause discomfort to wearer, and shall remain stowed until opened for use.  The hood shall fit over the Marine Corps helmet.  The jacket shall have sleeve pockets with pocket flaps that lie flat without curling edges and remain secure.  The sleeves shall have elasticized wrist openings with hook/loop tabs to adjust comfortably around wrist.  The underarms shall have pit zips to allow for venting.  The jacket shall have an attached rank tab on the front (see figure).

3.7.1.2 Trouser End Item Features (See Figure 2). The trouser center front waist closure shall be a durable and easy to fasten snap, with and an elasticized waist drawcord with barrel lock (ITW Nexus part #350-3000 or equal) for easy adjustment, to the body, with gloved hand.  The side seam pass through openings, with welts, shall allow direct access to trouser side pockets. The openings shall be secured closed with hook and loop at each end of the welt.  The elasticized trouser hem with hook/loop tabs shall adjust comfortably around boot upper.

3.7.2 Seaming.  Seaming shall be consistent, exhibit a uniform appearance and shall conform to the ASTM D-6193 stitch types.  The backside of all seams (inside garments) shall be flat with no protruding seam allowance or raw edges to create irritation or discomfort.  To maintain durability and functionality the seams shall be sewn with 10-14 stitches per inch for all outside visible stitching.  Overedge or pre-hemming shall be 6 – 10 stitches per inch.  All bartacks shall be 3/8 to 5/8 inch in length with approximately 27-28 stitches each and exhibit an overall peel strength of 25 lb.  Bartacks are required on zipper pulls. Bartack position will not prevent functioning of the zipper.  Material edges must not ravel.  All backstitching shall be 3/8” to ½” double back stitch. Raw edges may be turned-in, turned-under, surged, or seam sealed to prevent raveling.  No raw edges allowed.  The seat seam allowance must be sufficient so that the seam does not unravel or come unstitched.

4. VERIFICATION

4.1 Classification of inspection.  The inspection requirements specified herein are classified as follows:

1.  First article inspection (see 4.2)

2.  Quality conformance inspection (see 4.3)

4.2 First article inspection.  The first article, submitted in accordance with 3.1, shall be inspected for compliance with design, configuration, workmanship and dimensional requirements.  The presence of excessive defects, as defined by contract or failure to pass any test shall be cause for rejection of the first article.

4.3 Quality conformance inspection.  Sampling for inspection shall be performed in accordance with ANZI/ASQC Z1.4, inspection level shall be S-4, AQL 2.5.

  - Component and end item inspections.  In accordance with 4.1, components and end items shall be tested in accordance with all the requirements of referenced documents unless otherwise excluded, amended, modified, or qualified in this document or applicable procurement documents.  The government reserves the right to inspect all components and end items to determine conformance to requirements.

4.4.1 Material and Garment Testing. The cloth and/or garment shall be tested for the characteristics listed in Table I.  The testing shall be performed using the test methods as specified in table V.  All test reports shall contain the individual values utilized in expressing the final results.  For material testing, the sample unit shall be 5 continuous yards full width of the finished cloth, for all physical and chemical tests.  For garment testing, the sample unit shall be one jacket and one trouser per lot.  The lot shall be considered unacceptable if one or more sample units fail to meet any requirements specified.

      - Material testing. The materials shall be tested for the characteristics listed below.  The testing shall be performed using the test methods as specified.  All test reports shall contain the individual values utilized in expressing the final results.  The sample unit shall be 5 continuous yards full width of the finished cloth, for all tests.

#### Table IV. Test Methods

| Physical Property | Requirement Paragraph | Test Method |
| --- | --- | --- |
| Tear Strength; warp x filling | 3.3.2 | ASTM D- 2582 |
| Break Strength; warp x filling | 3.3.2 | ASTM D- 5034 (GE or GT) |
| Resistance to Organic Liquids after 5 launderings | 3.3.2 | AATCC 135 , 1/ and one drop of n-tetradecane for 30 seconds |
| Spray Rating after 5 launderings | 3.3.2 | AATCC 135 1/ and AATCC-22 |
| Water Permeability Fabric Seams After Accelerated Aging and creasing After –20 F Flex Fatigue; warp x filling After physical surface appearance After synthetic perspiration Blocking | 3.3.2 3.3.2 3.3.2 3.3.2 3.3.2 3.3.2 | ASTM D-751-06 (Procedure B2, 41-44) ASTM D-751-06: 72-79, followed by Procedure B2, 41-44 except fixed 50 cm water column/10 min. Aging conditions shall be 160 deg F for 7 days. ASTM F-392 (1000 cycles) & ASTM D-751-06 (Procedure B2,41-44) ASTM D-751-06:84-88 except the test shall be performed at 180 +/- 2 deg F for 30 minutes. 4/ and ASTM D-751-06 (Procedure B2, 41-44 except fixed 50 cm water column/10 min) 2/ and ASTM D-751-06 (Procedure B2, 41-44 except fixed 50 cm water column/10 min) |
| Dimensional Stability; warp x filling | 3.3.2 | AATCC–96, Option 1C |
| Hydrostatic Resistance Initial After strength of coating After High Humidity | 3.3.2 3.3.2 3.3.2 | ASTM D-751 (Procedure A, 37-40) ASTM D-751-06:72-29 (Desiccator with water in oven at 160 deg F for 7 days.) ASTM D-751-0672-79 (Desiccator with water in oven at 160 deg F for 7 days.) |
| Diethyltoluamide (DEET) Initial and after 5 launderings | 3.3.2 | Contaminate per 3/, laundered per AATCC 135 1/ and test per ASTM D-751 (Procedure A, 37-40) |
| Moisture Vapor Transmission | 3.3.2 | 6/ and ASTM E 96 B 6/ and ASTM E 96 Procedure BW |
| Visual Matching | 3.3.4.1 | AATCC Evaluation Procedure 9 |
| Colorfastness | 3.3.5 | AATCC Gray Scale for Color |
| Color | 3.3.6 | AATCC Evaluation Procedure 6 and 9 AATCC 8 AATCC 16 AATCC 61 |

4.4.2  Spectral Reflectance.  Finished cloth shall be meet requirements specified in 3.3.7.1.  Spectral reflectance shall be measured and reported on the initial cloth.  Certificate of compliance will be accepted on finished uniforms and subject to Government verification.    Spectral reflectance data shall be determined on the face side and shall be obtained from 600 to 860 nanometers (nm) at 20 nm intervals on a spectrophotometer relative to the barium sulfate standard, the preferred white standard.  Other white reference materials may be used provided they are calibrated to absolute white, e.g. magnesium oxide or vitrolite tiles.  The spectral bandwidth shall be less than 26 nm at 860 nm.  Reflectance measurements may be made by either the monochromatic or polychromatic mode of operation.  When the polychromatic mode is used, the spectrophotometer shall operate with the specimen diffusely illuminated with the full emission of a source that simulates either CIE source A or CIE source D65.  The specimen shall be measured as a single layer, backed with six layers of the same fabric and shade.  Measurements shall be taken on a minimum of two different areas and the data averaged.  The measured areas should be taken at least 6 inches away from the selvage.  The specimen shall be viewed at an angle no greater than 10 degrees from the normal, with the specular component included.  Photometric accuracy of the spectrophotometer shall be within 1 percent and the wavelength accuracy within 2 nm.  The standard aperture size used in the color measurement device shall be 0.3725 inches in diameter.  Any color having spectral reflectance values outside the limits at four or more of the wavelengths specified shall be considered a test failure.

4.4.3 Color Matching.

4.4.3.1   Visual color matching (all types and classes).  The color and appearance of the printed cloth shall match the standard sample when viewed using AATCC Evaluation Procedure 9, Option A, under filtered tungsten lamps that approximate artificial daylight D75 illuminant with a color temperature of 7500 ( 200 K with illumination of 100 ( 20 foot candles, and shall be a good match to the standard sample under horizon lamplight at 2300 ( 200 K.

4.4.3.2 Instrumental color matching (all types and classes).  Instrumental color matching is used as a tool to quantify shade evaluation.  Each measured color shall match the standard sample using AATCC Evaluation Procedure 6.  A color difference greater than a (E CMC = 1.5, when using a (E CMC  (2:1) ratio (D65 / 10() units as compared to the standard sample, shall be basis for rejection.

4.4.4 End item visual examination. The jacket and trouser shall be examined for the defects listed below.

| EXAMINATION | DEFECT |
| --- | --- |
| Material and workmanship | Component part omitted, distorted, full, tight, or twisted; any part caught in any unrelated stitching. |
|  | Any hole, cut, tear, smash, burn, drill hole, run, thin place, dye streak, color not as specified, misweave, knot or slub affecting appearance or serviceability |
| Material and workmanship | Seam: not type specified, puckered, distorted, pleated, wavy, twisted, irregular or open, loose or tight stitch tension, broken or missing thread or stitch, needle chew, visible mend, edge or raised stitching sewn too close to edge resulting in damage to cloth, seam allowance not as specified, visible raw edge - affecting appearance or serviceability. Seat seam not as specified. |
|  | Any component part omitted, not functioning properly, or defective. |
|  | Unwanted permanent fold, pleat, or crease in fabric or garments, affecting appearance or serviceability |
|  | Interlining bubbling, delaminating, bleed through, wrinkling, or puckering |
|  | Bartacks missing, insecure, misplaced, not specified size, stitches loose or broken, backtack not serving intended purpose. Bartack placement interferes with elastic stretch. Bartack at drawcord center point does not secure drawcord position. |
| Shade | Shade variation within a part or between parts. Unacceptable shade change as a result of water repellent treatment application. |
|  | Any color not as specified. |
| Cleanness | Spot, stain, excessive thread ends not trimmed or removed, shade stamp marking on outside; odor, affecting appearance or serviceability |
| Labels | Omitted, incorrect, illegible, not attached where specified; bar-codes omitted, not readable by scanner; human-readable interpretation (HRI) omitted or illegible; bar code not visible on folded, packaged item; bar code attachment causes damage to the item. |
| Packaging | Not packaged in accordance with the contract or purchase order. |

4.4.5 Finished dimensions.  The jacket and trouser shall conform to the dimensions listed in Table V below:

###### Table V. Jacket and Trouser Finished Dimensions

|  | JACKET * | TROUSER * |
| --- | --- | --- |
| Size | 1/2 Chest 1/ | Back Length 2/ | Sleeve Length 3/ | 1/2 Waist 4/ | Inseam 5/ | Outseam 6/ |
| Small Short | 24 | 29 ¾ | 24 ¼ | 18 | 30 | 40 ½ |
| Small Regular | 24 | 30 ¼ | 25 ¼ | 18 | 32 | 44 |
| Medium Short | 26 | 30 ¼ | 24 ½ | 19 | 30 | 42 |
| Medium Regular | 26 | 30 ¾ | 25 ½ | 19 | 32 | 44 |
| Medium Long | 26 | 33 ¼ | 26 ¼ | 19 | 34 | 47 |
| Large Regular | 28 | 31 ¼ | 25 ¾ | 20 | 32 | 45 |
| Large Long | 28 | 33 ¾ | 26 ½ | 20 | 34 | 47 |
| X-Large Long | 30 | 34 ¼ | 26 ¾ | 22 | 34 | 47 |
| Tolerance | +/-3/4” | +/- 3/4” | +/- 3/4” | +/- 3/4” | +/- 3/4” | +/- 3/4 ” |

Note: ADD IN VELCRO SIZE

* Dimensional Measurements: All garments shall be measured under relaxed condition where zippers are closed and hook/loop tabs are engaged without cinching.  Closed garments are smoothed gently to lie flat. Measurements shall be taken in a straight line.

1/ Measure across the chest from flattened folded edge to flattened folded edge at the base of the armhole seams.

2/ Measure from center of neck seam stitch line to bottom edge of hem.

3/ Measure from top of armhole seam where it intersects with shoulder seam to bottom edge of the sleeve hem.

4/ Straighten the waist without stretching and measure across the center of the waistband between folded side edges.

5/ Position trousers with inseam facing up, smooth, and flat.  Measure from center seat back seam where it intersects with inseam to the bottom edge of leg elasticized hem.

6/ Orient trousers so that trouser legs are parallel, and lying flat and smooth. Measure from top edge of waistband along outseam to bottom edge of leg elasticized hem.

5.  PACKAGING

5.1 Packaging.  For acquisition purposes, the packaging requirements shall be in accordance with best commercial practice and ASTM D- 3951 unless specified differently in the contract or purchase order (see 6.2).  Each item shall be packaged separately with no mixed cartons.  Partial cartons will be clearly marked. When actual packaging of material is to be performed by DoD personnel, these personnel need to contact the responsible packaging activity to ascertain requisite packaging requirements.  Packaging requirements are maintained by the Inventory Control Point's packaging activity within the Military Department's System Command.  Packaging data retrieval is available from the managing Military Department or Defense Agency's automated packaging files, CD-ROM products, or by contacting the responsible packaging activity.

6.  NOTES

(This section contains information of a general or explanatory nature that may be helpful, but is not mandatory.)

6.1 Intended use.  The extreme cold weather uniform is for wear by military personnel of the United States Marine Corps when additional warmth in extreme cold is required.

6.2 Acquisition requirements.  Acquisition documents should specify the following:

a.  Title, number and date of this document.

b.  Types, classes and sizes required (see 1.2).

c.  Issue of DODISS to be cited in the solicitation and, if required, the specific issue of 
 individual documents referenced (see 2.2.1 and 2.3).

d.  When first article sample is required (see 3.1, 4.2 and 6.3).

e.  Packaging requirements (see 5.1)

6.3 First article.  When a first article is required, it shall be inspected and approved under the appropriate provisions of FAR 52.209-4.  The first article should be a preproduction sample.  The contracting officer should specify the appropriate type of first article and the number of units to be furnished.  The contracting officer should include specific instructions in all acquisitions documents regarding arrangements for selection, inspection, and approval of the first article.

  - Sources of Supply.

W.L.Gore & Associates

105 Vieves Way

Elkton, MD  21922-0729

Phone Number: 410-506-5000

Propper International Inc.

520 Huber Park Court

St. Charles, MO 63304

Phone Number: 636-685-1073

Cord Closure:

ITW Waterbury Buckle

Waterbury, Connecticut 06706

Phone Number: 401-225-8251

Velcro USA Inc.
406 Brown Avenue
Manchester, NH 03103
Tel: (800) 225-0180
Fax: (603)669-92

Jason Mills

349 Kinderkamack Road

Westwood, NJ 07675

(201) 358-6500

6.5 Subject term (key word) listing.

Uniform

Clothing

Water repellent

6.6 Figures.

6.6.1 Figure 1: Light Weight Exposure Suit Jacket.  Jacket front view, pocket and hood detail.

6.6.2 Figure 2: Lightweight Exposure Suit Jacket, Stow-able Hood.  Stow-able hood shown from back view of jacket.  Collar folded down view, collar flipped up view.

6.6.3 Figure 3: Lightweight Hardshell Trouser.  Trouser front view, gusset detail, and trouser side view.